ABSTRACT

PROCESS OF STIRRING ROD AND FIN MAKING OF STIRRING-MACHINE

OF BIOGAS DIGESTER

By:

Khanifudin

09508131018

Process of stirring rod and fin making of stirring-machine of biogas digester as a mean to (1) knowing the material that is needed in the process of stirring and fin making of stirring-machine of biogas digester, (2) knowing the tools that is needed in the process of stirring rod and fin making of biogas digester, (3) knowing process of the stirring rod and fin making of biogas digester that is valuable, powerful and efficient, (4) knowing workability of the process of stirring rod and fin making of stirring-machine of biogas digester.

Process of agitator rod and fin making of stirring-machine of biogas digester include (1) identification of the material that is needed for making stirring rod and fin of the stirring-machine of biogas digester, (2)  selection tools that is used in the process stirring rod and fin of the stirring-machine of biogas digester, (3)  the process of stirring rod and fin making of stirring-machine of biogas digester, (4) workability of the process of stirring rod and fin making of stirring-machine of biogas digester.

This process by means of many stage, include (1) identification of the material that is used, they have to strong and resilient, so the material that is used as stirring-rod use pipe with measure ø20mm x 600mm whereas the fin of agitator use the plat eyser with the thickness 3mm, (2) the tools that is used to make the fin and the rod of agitator of biogas digester are welding machine SMAW, offhand grinding, grinding machine cutting, band saw machine, slide gauge, angle ruler, punch, scriber, ruler steel, pinchers, plate-cutter, sand-paper, wrench with measure 19mm, slag hammer, steel brush, clamp C, (3a) the process of the agitator rod making include cutting plan of the pipe, the process of cutting, boring ø10 mm, the assembling of nut to the agitator  rod, finishing, (3b) the process of the agitator fin include cutting plan of the plate, the process of cutting the material, the assembling of the agitator fin, finishing, (3c) the assembling of the agitator rod and fin with fitting the nut and the bolt at the agitator rod and agitator rod, (4) testing of the workability of the agitator rod and fin at the stirring-machine of biogas digester, the rod and fin can be stirring the dumpling best, powerful in the construction, capable to quicken the process of banishment the rest of the dung that it is not to be used.

Keyword: agitator rod and agitator fin, biogas