SINTESIS DAN BIODEGRADASI POLIURETAN HASIL SINTESIS DARI ASAM LEMAK MINYAK KELAPA SAWIT (CPO), POLIOKSIETILEN GLIKOL 400 (PEG 400), DAN METILEN -4,4'-DIFENILDIISOSIANAT (MDI)

Oleh: 
Sihweni Koniawati 
04307141021
ABSTRAK

Penelitian ini dilakukan dengan tuiuan untuk mempelajari karakter poliuretan hasil sintesis dari asam lemak CPU, PEG 400, dan MDI, mengetahui pengaruh penggunaan asam lemak CPO hasil oksidasi terhadap ikatan silang poliuretan hasil sintesis, mempelajari pengaruh proses oksidasi terhadap kemudahan biodegradasi poliuretan hasil sintesis, mempelajari pengaruh waktu inkubasi terhadap kehilangan massa poliuretan hasil sintesis serta mempelajari pengaruh waktu inkubasi terhadap biodegradabilitas poliuretan hasil sintesis.

Pada penelitian ini poliureatan diperoleh dari polimerisasi antara asam lemak CPO, polioksietilen glikol 400, dan metilen-4,4'-difenildiisosianat pada temperatur kamar diikuti dengan pemanasan pada suhu 120oC selama 1 jam. Karakterisasi poliuretan dilakukan melalui penentuan gugus fungsi dengan Fourier Transform Infra Red, penentuan ikatan silang, serta analisis kristalinitas poliuretan dengan menggunakan X-Ray Diffraction. Biodegradasi poliuretan dilakukan dengan menggunakan mikroorganisme yang berasal dari lumpur aktif serta media malka padat pada temperatur 37°C. Variasi waktu inkubasi berturut-​turut adalah 5, 10, 15, 20, 25, dan 30 hari, dengan penggantian media setiap 5 hari.

Poliuretan hasil sintesis dari asam lemak CPO + PEG 400 + MDI muncul serapan spektrum FTIR yang menunjukkan gugus fungsi uretan pada 1646,15 cm​1 dan 1645,98 cm-1 masing-masing untuk poliuretan sebelum dan sesudah biodegradasi. Derajat penggembungan poliuretan dari asam lemak CPO + PEG 400 + MDI adalah 44,175 %. Derajat kristalinitas poliuretan dari asam lemak CPO + PEG 400 + MDI sebelum biodegradasi adalah 48,794 %, sedangkan derajat kristalinitas poliuretan dari asam lemak CPO + PEG 400 + MDI sesudah biodegradasi adalah 48,626 %. Poliuretan hasil sintesis dari asam lemak CPO teroksidasi + PEG 400 + MDI muncul serapan yang menunjukkan gugus fungsi uretan pada 1646,49 cm" dan 1647,31 cm-1 masing-masing untuk poliuretan sebelum dan sesudah biodegradasi. Derajat penggembungan poliuretan dari asam lemak CPO teroksidasi adalah 69,701 %. Derajat kristalinitas poliuretan dari asam lemak CPO teroksidasi + PEG 400 + MDI sebelum biodegradasi adalah 52,825 %, sedangkan derajat kristalinitas poliuretan dari asam lemak CPO teroksidasi + PEG 400 + MDI sesudah biodegradasi adalah 48,957 %.

SYNTHESIS AND BIODEGRADATION OF POLYURETHANES OF SYNTHESIS RESULTS FROM FATTY ACIDS IN CRUDE PALM OIL (CPO), POLIOKSIETILEN GLIKOL 400 (PEG 400), AND METILEN -4, 4'-DIFENILDIISOSIANAT (MDI)
By:

Sihweni Koniawati

04307141021

ABSTRACT

This research aims at studying polyurethanes of synthesis results from fatty acids in CPO, PEG 400, and MDI; determining the effect of the use of fatty acids in CPO of oxidation results on the cross linking of polyurethanes of synthesis results; studying the effect of oxidation to the ease of biodegradation of polyurethanes of synthesis results; studying the effect of incubation times on the mass loss of polyurethanes of synthesis results; and studying the effect of incubation times on the biodegradability of polyurethanes of synthesis results. 
In this study, polyurethanes were obtained from the polymerization between fatty acids in CPO, polioksietilen glikol 400, and metilen-4, 4'-difenildiisosianat at room temperature followed by heating at the temperature of 120°C for one hour. Characterization of polyurethanes was done through the determination of functional groups by Fourier Transform Infra Red, the determination of the cross linking, and the polyurethane crystallinity analysis by using X-Ray Diffraction. Biodegradation of polyurethanes was performed using microorganisms from activated sludge and solid Malka at the temperature of 37°C. Variation of incubation times consisted of 5, 10, 15, 20, 25, and 30 days, with media replacement of every 5 days. 
In the polyurethanes of synthesis results from fatty acids in CPO + PEG 400 + MDI, FTIR spectra absorption appeared showing the urethane functional group at 1646.15 cm​1 and 1645.98 cm-1 and each for polyurethanes before and after biodegradation. The degree of the polyurethanes’ swelling from fatty acids in CPO + PEG 400 + MDI was 44.175%. The degree of crystallinity of polyurethanes from fatty acids in CPO + PEG 400 + MDI before biodegradation was 48.794%, while the degree of the polyurethanes’ crystallinity from fatty acids in CPO + PEG 400 + MDI after biodegradation was 48.626%. In polyurethanes of synthesis results from oxidized fatty acids in CPO + PEG 400 + MDI, the absorption of urethane functional group appeared at 1646.49 cm​1 and 1647.31 cm-1, each for the polyurethanes before and after biodegradation. The swelling degree of polyurethanes of oxidized fatty acids in CPO was 69.701%. The degree of crystallinity of polyurethanes of oxidized fatty acids in CPO + PEG 400 + MDI before biodegradation was 52.825%. Meanwhile, the degree of crystallinity of polyurethanes of oxidized fatty acids in CPO + PEG 400 + MDI after biodegradation was 48.957%.

