PEMISAHAN ION LOGAM ZINK (II) DALAM LIMBAH CAIR

PENYAMAKAN KULIT SECARA EMULSI MEMBRAN CAIR

Oleh:

Surwidia Ningsih

033314033

Pembimbing Utama		: Regina Tutik Padmaningrum, M.Si

Pembimbing Pendamping	: Sunarto, M.Si

ABSTRAK

Penelitian ini dilakukan di laboratorium Kimia FMIPA UNY dan UII. Tujuan penelitian ini adalah (1) mengetahui persentase (v/v) optimum surfaktar. (Span 80). (2) konsentrasi fasa internal (larutan NH4OH), (3) waktu optimum pengadukan selama ekstraksi ion zink(II), (4) persen ekstraksi ion logam zink(II) dalam limbah cair penyamakan kulit pada keadaan optimum dan (5) konsentrasi ion logam zink(II) yang terekstraksi dalam limbah cair penyamakan kulit dengan metode emulsi membran cair.

Subjek dalam penelitian ini adalah limbah cair penyamakan kulit, sedangkan objek penelitiannya adalah pemisahan ion logam zink(II). Persentase volum surfaktan optimum ditentukan dengan cara menvariasikan % v/v surfaktan sebesar 1, 3, 5, 7, dan 9%. Kosentrasi fasa internal (NH40H) optimum ditentukan dengan eara menvariasikan konsentrasi larutan NH4OH sebesar 0.5, 0.75, 1.0, 1.25, dan 1.5 M. Fasa membran terdiri dari sorbitan monooleat (Span 80) sebagai surfaktan, trietilamin (TEA) sebagai zat pembawa clan kerosen sebagai pelarut. Proses pemisahan dilakukan dengan metode emulsi membran cair yaitu gabungan ekstraksi dan reekstraksi dalam suatu proses yang berlanjut. Campuran fasa membran dan fasa internal tersebut kemudian diaduk dengan kecepatan 1200 rpm selama 10 menit. Emulsi yang terbentuk dikontakkan dengan limbah cair penyamakan kulit dengan perbandingan volum (1:1), dibuat 3 macam campuran dengan volume sama lalu diaduk dengan kecepatan 300 rpm selama 5, 10, dan 15 menit untuk masing-masing campuran.

Hasil penelitian menunjukkan bahwa (1) persentase (v/v) optimum surfaktan adalah 9 %, (2) konsentrasi optimum fasa internal (NH40H) adalah 1.0 M, (3) waktu pengadukan selama ekstraksi ion logam zink(II) adalah 10 menit, (4) persentase ekstraksi ion logam zink(II) dalam limbah cair penyamakan kulit pada keadaan optimum sebesar 93.761 % dan (5) konsentrasi ion logam zink(II) yang terekstraksi dalam limbah cair penyamakan kulit sebesar 0.1889 ppm.

SEPARATION OF ZINK (II) METAL IONS IN TANNERY WASTEWATER BY EMULSION LIQUID MEMBRANE

By: 
Surwidia Ning 
033314033

First consultant	: Regina Tutik Padmaningrum, M. Si

Second consultant	: Sunarto, M. Si

ABSTRACT

This research was conducted in the Laboratory of Chemistry of Faculty of Mathematics and Natural Sciences (FMIPA)-Yogyakarta State University (UNY) and in the Chemistry Laboratory of Islamic University of Indonesia (UII). The purpose of this study was to determine (1) the optimum percentage of (v/v) of surfactant (Span 80), (2) the concentration of internal phase (solution of NH40H), (3) the optimum stirring time during the extraction of zinc (II) ions, (4) the percentage of extraction of zinc (II) metal ions in tannery wastewater in optimum condition, and (5) metal ion concentration of zinc (II) extracted in tannery wastewater by emulsion liquid membrane method.

The subject of the study was tannery wastewater, while the research object was the separation of zinc (II) metal ions. Percentage of optimum volume of surfactant was determined by varying the percentage of v / v of the surfactant at 1, 3, 5, 7, and 9%. The optimum concentration of the internal phase (NH40H) was determined by varying the concentration of NH40H solution of 0.5, 0.75, 1.0, 1.25, and 1.5 M. The membrane phase consisted of sorbitan monooleate (Span 80) as surfactant, triethylamine (TEA) as carrier substance and kerosene as solvent. The separation process was conducted using liquid membrane emulsion which was combination of extraction and re-extraction in the ongoing process. Mixture of membrane phase and internal phase was then stirred with a speed of 1200 rpm for 10 minutes. Emulsion formed was contacted with tannery wastewater using the volume ratio (1:1), made into 3 kinds of mixture with the same volume, and then stirred at 300 rpm for 5, 10, and 15 minutes for each mix.

Research results showed that (1) the surfactant optimum percentage of (v / v) was 9%, (2) the optimum concentration of the internal phase (NH40H) was 1.0 M, (3) the stirring duration during the extraction of metal ions of zinc (II) was 10 minutes, (4) the extraction percentage of metal ions of zinc (II) in tannery wastewater at an optimum state was 93.761%, and (5) the metal ion concentration of zinc (II) extracted in the tannery effluent was 0.1889 ppm.