PENGARUH VARIASI VOLUME LARUTAN NANOPARTIKEL PERAK DENGAN KONSENTRASI 5 mM TERHADAP POROSITAS DAN KUAT TEKAN MORTAR

Oleh:

Happy Susi Agus Tina

11306141008

ABSTRAK

Seiring dengan pesatnya perkembangan pembangunan, manusia membutuhkan  kualitas bahan bangunan yang lebih baik seperti mortar. Untuk meningkatkan kualitas mortar maka diberikan suatu produk yang dapat meningkatkan kualitas mortar, yaitu Nanosilver. Tujuan dari penelitian ini ialah untuk mengetahui pengaruh  larutan nanopartikel perak dengan konsentrasi 5 mM terhadap porositas dan kuat tekan mortar, mengetahui pengaruh variasi volume larutan nanopartikel perak dengan konsentrasi 5 mM terhadap porositas dan kuat tekan mortar, mengetahui volume larutan nanopartikel perak yang dapat memberikan pengaruh secara maksimal terhadap porositas dan kuat tekan mortar, dan mengetahui pengaruh lamanya perendaman terhadap porositas dan kuat tekan mortar.

Bahan dari penelitian ini adalah perak nitrat (AgNO3), trisodium sitrat (Na3C6H5O7), dan aquades. Penelitian ini dimulai dengan membuat larutan perak nitrat (AgNO3) dan larutan trisodium sitrat (Na3C6H5O7). Selanjutnya nanopartikel perak disintesis menggunakan metode bottom-up dengan konsentrasi 5 mM. Menguji absorbansi nanopartikel perak dengan menggunakan spektrofotometri UV-Vis. Nanopartikel perak ditambah ke dalam mortar dengan variasi 0 ml, 5 ml,10 ml,15 ml, 20 ml, dan 25 ml selanjutnya menguji porositas, kuat tekan dan kandungan unsur dalam mortar.

Penambahan nanopartikel perak 5 mM pada mortar memberikan pengaruh terhadap porositas dan kuat tekan mortar. Sebagian besar hasil menunjukkan semakin besar volume penambahan nanopartikel perak pada mortar memberikan penurunan porositas dan peningkatan kuat tekan pada mortar. Volume nanopartikel perak 5 mM yang memberikan pengaruh secara maksimal terhadap mortar ialah  penambahan nanopartikel sebanyak 5 sampai 15 ml. Perendaman selama empat minggu memberikan kekuatan yang maksimal terhadap porositas dan kuat tekan mortar.

Kata kunci:  nanopartikel perak, mortar, porositas, kuat tekan.

THE INFLUENCE OF THE VARIATION OF SILVER NANOPARTICLE SOLUTION VOLUME WITH  5 mM CONCENTRATION TOWARDS THE POROSITY AND COMPRESSIVE STRENGTH OF MORTAR

By:

Happy Susi Agus Tina

11306141008

ABSTRACT

As the world is growing rapidly, people need better building materials such as mortar. In order to increase the quality of mortar being used in the research, the mortar is made by adding silver nanoparticle in it. The aim of this research is to determine the effect of silver nanoparticle with concentrate 5 mM towards the porosity and compressive strength of mortar, to determine the effect  volume variation of silver nanoparticle with concentrate 5 mM towards the porosity and compressive strength of mortar, determine the solution volume of silver nanoparticle that can give effect maximally towards the porosity and compressive strength of mortar, and to determine the effect of submersion time to porosity and compressive strength of mortar.

The substance of this research is silver nitrate (AgNO3), trisodioum citrate (Na3C6H5O7) and aquades. This research was started by making the solution of nitrate silver (AgNO3) and trisodium citrate. Then, the silver nanoparticle is synthesis by using bottom-up method with concentrate 5 mM. The absorbance was determined by spectrophotometer Uv-Vis. In the next step, the silver nanoparticle is added to the varied mortar with volume variations of 0 ml, 5 ml, 10 ml, 15 ml, 20 ml, and 25 ml. Then determine porosity, compressive strength, and the content of mortar.

By the adding silver nanoparticle solution with concentrate 5 mM in mortar can give effect towards the porosity and compressive strength of mortar. A half of them show that more bigger adding volume of silver nanoparticle solution to mortar gives the decrease to porosity and icrease to compressive strength. Volume silver nanoparticle solution with concentrate 5 mM that can gives the maximal effect towards the porosity and compressive strength of mortar was silver nanoparticle solution volumes of 5 up to 15 ml. Submersion for four weeks can gives the maximal effect towards the porosity and compressive strength of mortar.

Keywords: silver nanoparticle, mortar, porosity, compres