PENGARUH ADSORBEN GOETHIT DAN ALUMINA

TERHADAP ADSORPSI ION FOSFAT

Oleh  :

Budi Setiawan

04307144016

Pembimbing Utama		: Jaslin Ikhsan, Ph.D

Pembimbing Pendamping	: Dr. Endang Widjajanti LFX

ABSTRAK

Penelitian ini bertujuan untuk mengetahui pengaruh berbagai luas permukaan terhadap adsorpsi ion fosfat pada adsorben goethit dan alumina, mengetahui pengaruh pH sistem terhadap adsorpsi ion fosfat oleh berbagai luas permukaan pada adsorben goethit dan alumina dan mengetahui perbandingan daya adsorpsi ion fosfat antara adsorben goethit dan alumina.

Adsorben goethit dan alumina sebelum digunakan dalam penelitian dilakukan beberapa analisis antara lain: analisis luas permukaan surface areameter untuk mengetahui luas permukaan spesifik, analisis XRD dan IR digunakan untuk menentukan kemurnian adsorben. Dalam menentukan adsorpsi ion fosfat dilakukan tiga eksperimen yaitu proses adsorpsi tepi dilakukan dengan konsentrasi adsorben 25, 50 dan 100 m2iL pada rentang pH antara 3-10 dengan konsentrasi fosfat 0,001 M yang dilakukan pada suhu 30°C, proses kinetika adsorpsi dilakukan pada luas permukaan 25 m2/L dengan menggunakan pH maksimum pada waktu dari menit ke 5 s/d 2910 dan suhu 30°C dan proses kinetika desorpsi dilakukan pada luas permukaan 25 mz/L dengan cara pH dinaikkan menjadi pH maksimum kemudian pH diturunkan menjadi pH minimum pada waktu dari menit ke 5 s/d 2910 dan suhu 30°C, cara menentukan % adsorpsi ion fosfat dilakukan menggunakan spektrometer UV-VIS dan Identifikasi fosfat yang terjerap menggunakan spektrometer IR. Perbandingan % adsorpsi ion fosfat adsorben goethit dan alumina dianalisis dengan cara kuntitatif menggunakan uji-t.

Hasil penelitian ini menunjukan bahwa variasi luas permukaan terhadap adsorpsi ion fosfat oleh sorben goethit dan alumina yaitu prosentase maksirnum fosfat teradsorpsi sebanding pada luas permukaan dalam penelitian, pH sistem berpengaruh terhadap adsorpsi ion fosfat oleh sorben goethit dan alumina dan Perbandingan % adsorpsi ion fosfat antara sorben goethit dan alumina pada eksnerimen adsorpsi tepi, kinetika adsorpsi dan kinetika desorpsi menunjukan adanya perbedaan signifikan yang berarti adanya perbedaan % adsorpsi ion fosfat antara sorben goethit dan alumina.

EFFECTS OF GOETHIT AND ALUMINA ADSORBENTS

TOWARDS PHOSPHATE ION ADSORPTION

By:

Budi Setiawan

04307144016

First consultant	: Jaslin Ikhsan, Ph.D

Second consultant	: Dr. Endang Widjajanti LFX

ABSTRACT

This study aims at determining (1) effects of various surface areas towards phosphate ion adsorption in goethit and alumina adsorbents, (2) effects of system pH towards phosphate ion adsorption by various surface areas in goethit and alumina adsorbents, and (3) comparison on the adsorption capacity of the phosphate ion between goethit and alumina adsorbents.

Before using goethit and alumina adsorbents in this reserach, there were some analyses done including an analysis of surface areameters to determine a specific surface area and XRD and IR analysis used to determine the adsorbent purity. In determining the phosphate ion adsorption, three experiments were conducted. The first experiment was the edge adsorption process conducted using adsorbent concentrations of 25, 50, and 100m2/L at pH ranges of 3 to 10 with the phosphate concentration of 0.001 M conducted at the temperature of 30°C. The second one was the adsorption kinetics process conducted at the surface area of 25 m2/L using a maximum pH at the time of 5 to 2910 minutes and at the temperature of 30°C. The last experiment was the desorption kinetics process conducted at the surface area of 25 m2/L using pH increased to the maximum pH, then, decreased to the minimum pH at the time of 5 to 2910 minutes and at the temperature of 30°C. Percent (%) of phosphate ion adsorption was determined by using UV-VIS spectrophotometer and the adsorbed phosphate identification using IR spectrophotometer. The comparison of phosphate ion adsorption percent of goethit and alumina adsorbents was analyzed by using Quantitative method with the t-test.

The research results showed that various surface areas on phosphate ion adsorptions by goethit and alumina adsorbents i.e. the maximum percentage of the adsorbed phosphate was equal to the surface area in the research, system pH influenced on the phosphate ion adsorption by goethit and alumina sorbents, and the % comparison of the phosphate ion adsorption between goethit and alumina sorbents in the experiments of edge adsorption, kinetics adsorption, and kinetics desorption showed significant differences meaning that there was % difference on the phosphate ion adsorption between goethit and alumina sorbents.