POLA ADSORPSI ZEOLIT TERHADAP PEWARNA 
AZO METIL MERAH DAN METIL JINGGA
Oleh:

Endang Widjajanti,

Regina Tutik P, dan

M. Pranjoto Utomo

ABSTRAK

Penelitian ini bertujuan untuk 1) menentukan pH sistem optimum untuk adsorpsi pewarna azo metil merah dan metil jingga, 2) menentukan waktu adsorpsi optimum untuk adsorpsi zeolit terhadap pewarna azo metil merah dan metil jingga pada kondisi pH optimum dan 3) menentukan pola adsorpsi zeolit terhadap pewarna metil merah maupun metil jingga. 

Sebagai subyek penelitian adalah zeolit alam, sedangkan objek penelitian ini adalah daya adsorpsi zeolit terhadap pewarna metil merah (MR) dan metil jingga (MO). Sedangkan variabel bebas adalah pH, waktu adsorpsi dan konsentrasi pewarna, Optimasi rasio massa adsorben dan adsorbat dilakukan dengan menambahkan pada 50 mL larutan pewarna metil merah sejumlah tertentu zeolit, tanpa pengaturan pH. Optimasi pH dilakukan pada kondisi massa optimum dengan waktu adsorpsi 24 jam dan konsentrasi pewarna 20 ppm. Waktu adsorpsi ditentukan pada kondisi massa dan pH optimum, sedangkan variasi konsentrasi dilakukan pada kondisi massa, pH dan waktu optimum. Daya adsorpsi ditentukan dengan membandingkan konsentrasi pewarna sebelum dan sesudah adsorpsi. Konsentrasi pewarna dilakukan menggunakan spektrofotometer sinar tampak pada panjang gelombang maksimumnya. Karakterisasi zeolit ditentukan secara FTIR. 

Hasil penelitian memperlihatkan bahwa 1) hasil optimasi pH pada adsorpsi zeolit terhadap pewarna metil merah maupun metil jingga didapatkan pH optimum adalah 2, 2) waktu optimum untuk adsorpsi adsorpsi zeolit terhadap pewarna metil merah maupun metil jingga adalah sama yaitu 60 menit dan 3) Adsorpsi zeolit terhadap pewarna metil merah mengikuti pola isoterm Freundlich. 

Kata kunci : Adsorpsi, Zeolit, pewarna Azo 
ZEOLITE ADSORPTION PATTERNS ON 
AZO DYE METHYL RED AND DYE METHYL ORANGE 
By:

Endang Widjajanti,

Regina Tutik P, and

M. Pranjoto Utomo

ABSTRACT

This study aims at determining (1) the optimum pH of system for the adsorption of azo dye methyl red and dye methyl orange, (2) the optimum adsorption time of the zeolite adsorption of azo dye methyl red and dye methyl orange at the optimum pH, and (3) the patterns of zeolite adsorption of the dye methyl red and dye methyl orange. 

The research subject was the natural zeolite, while the object of this research was zeolite adsorption capacity of dye methyl red (MR) and dye methyl orange (MO). The independent variables were pH, adsorption time, and concentration of dye. Optimization of the mass ratio of adsorbent and adsorbate was done by adding certain amount of zeolite to 50 mL of solution of red methyl dye, without pH regulation. Optimization of pH was carried out under conditions of the optimum mass with 24-hour adsorption time and the dye concentration of 20 ppm. The adsorption time was determined at the optimum mass and pH conditions, while the variation of concentration was carried out under the optimum mass, pH and time conditions. Adsorption capacity was determined by comparing the concentration of dye before and after adsorption. The concentration of dye was carried out using a visible light spectrophotometer in its maximum wavelength. Characterization of zeolite was determined by FTIR. 

The results showed that (1) the optimization of pH on the adsorption of zeolite to the dye methyl red and dye methyl orange obtained the optimum pH of 2, (2) the optimum time for zeolite adsorption of dye methyl red and dye methyl orange was the same (60 minutes), and (3) the adsorption of zeolite of dye methyl red followed the Freundlich isotherm pattern. 

Keywords: Adsorption, Zeolite, Azo dyes

