OPTIMASI POTENSIAL, SUHU LARUTAN, DAN PENGARUH PENGADUKAN PADA ELEKTRODEPOSISI ION LOGAM Ag(I) DALAM LIMBAH CAIR ELEKTROPLATING DENGAN AGEN PEREDUKSI

FORMALDEHIDA

Oleh:

Abdul Fikar Amigato

09307144008

| Pembimbing Utama Pembimbing Pendamping | : Siti Marwati, M.Si : Regina Tutik Padmaningrum, M.Si |
| --- | --- |

ABSTRAK

Penelitian ini dilakukan di Laboratorium Penelitian Kimia FMIPA Universitas Negeri Yogyakarta (UNY). Tujuan penelitian ini adalah untuk menentukan potensial dan suhu larutan optimal, pengaruh pengadukan pada proses elektrodeposisi ion logam Ag(I) dalam limbah cair elektroplating serta pengaruh formaldehida terhadap karakteristik deposit Ag.

Subjek penelitian ini adalah limbah cair elektroplating yang diambil dari sentra kerajinan perak Kotagede Yogyakarta. Objek penelitian adalah efisiensi elektrodeposisi pada variasi potensial dan suhu. Proses elektrodeposisi dilakukan dengan variasi potensial; suhu larutan; dan perlakuan pengadukan. Konsentrasi Ag(I) hasil elektrodeposisi dianalisis dengan metode Spektrofotometri Serapan Atom. Kualitas deposit Ag ditentukan dengan pengamatan secara visual. Struktur kristal hasil elektrodeposisi ditentukan dengan metode Difraksi Sinar-X.

Hasil penelitian menunjukkan bahwa: 1) potensial optimal sebesar 5 volt dengan efisiensi elektrodeposisi yaitu 40,887%; 2) suhu optimal 500C dengan efisiensi elektrodeposisi yaitu 41,905%; 3) adanya perlakuan pengadukan dapat memperbesar efisiensi elektrodeposisi yaitu 48,556%; dan 4) deposit Ag hasil elektrodeposisi dengan penambahan formaldehida lebih kristalin dengan parameter kisi rata-rata 4,0751 Å dibandingkan dengan tanpa penambahan formaldehida dengan perameter kisi rata-rata 4,0553 Å.

Kata kunci: ion logam Ag(I), elektrodeposisi, formaldehida, limbah cair elektroplating

OPTIMIZED VOLTAGE, SOLUTION TEMPERATURE, AND EFFECT OF STIRRING ON THE ELECTRODEPOSITION ION SILVER Ag(I)

IN ELECTROPLATING LIQUID WASTE BY

FORMALDEHIDE REDUCING AGENTS

By:

Abdul Fikar Amigato

09307144008

| Supervisor Co-Supervisor | : Siti Marwati, M.Si : Regina Tutik Padmaningrum, M.Si |
| --- | --- |

ABSTRACT

This research was done at Chemistry Research Laboratory of FMIPA Yogyakarta State University (UNY). The aims of this research were to determine optimum voltage, solution temperature, effect of stirring electrodeposition process Ag(I) ion in electroplating liquid waste, and the effect of formaldehyde on characteristics of Ag deposit.

The subject of this research was electroplating liquid waste were taken from silver centers at Kotagede Yogyakarta. The object was electrodeposition efficiency by varying the voltage and temperature. Electrodeposition was done with a varying of voltage; solution temperature; and effect of stirring. Ag(I) concentration of the electrodeposition result was analyzed by using Atomic Absorption Spectrophotometry method. The quality of silver deposit was done by visual observation. The crystal structure of the electrodeposition result was determined by the X-Ray Diffraction method.

The result of this research showed that: 1) optimum voltage of 5 volt with the electrodeposition efficiency 40.887%; 2) optimum temperature of 500C with the electrodeposition efficiency 41.905%; 3)  the existance of stirring can increase the efficiency of the electrodeposition 48.556%; 4) Ag deposit electrodeposition result with the formaldehyde produced was more crystalline with the lattice parameter on average 4.0751 Å compared with no addition of formaldehyde with the lattice parameter on average 4.0553 Å.

Keywords : Ag(I)ion, electrodeposition, formaldehyde, electroplating liquid waste