SINTESIS NANOPARTIKEL PbS MELALUI METODE SOL-GEL

DENGAN ASAM ETILEN DIAMIN TETRAASETAT (EDTA)

SEBAGAI CAPPING AGENT

Oleh:

Bintang Tunjung Sari

11307141025

Pembimbing: Dr. Cahyorini Kusumawardani, M.Si

ABSTRAK

Penelituan ini bertujuan untuk mengetahui pengaruh variasi penambahan EDTA terhadap ukuran partikel dan karakter elektronik pada material PbS. Nanopartikel PbS dengan capping agent EDTA  disintesis dengan metode sol-gel dengan prekusor Pb(CH3COO-)2 sebagai sumber Pb dan (NH4)2S sebagai sumber S serta EDTA sebagai capping agent. Konsentrasi EDTA yang digunakan antara lain: 0 mmol; 0,1 mmol; 0,2 mmol; 0,5 mmol; 1 mmol. Proses sol-gel dilakukan dengan mengaduk CTAB, SDS dan EDTA sampai homogen, kemudian ditambahkan Pb(CH3COO-)2 dan (NH4)2S dan diaduk selama 5 menit untuk menghasilkan endapan PbS berwarna hitam. Endapan disaring kemudian dioven pada suhu 120oC selama 3 jam. Hasil XRD menunjukkan bahwa struktur PbS adalah kubik, dengan ukuran masing masing 8,99 nm; 2,36 nm; 12,7889 nm; 12,5650 nm; 21,8003 nm. Sedangkan hasil karakterisasi dengan   UV-Vis menghasilkan nilai energi celah pita untuk PbS/EDTA masing masing 3,2 eV; 3,3 eV; 2,8 eV; 2,8 eV dan 2,3 eV.

Kata kunci: nanopartikel, sel surya, EDTA, capping agent

NANOPARTICLE SYNTHESIS OF PbS BY SOL-GEL METHOD

WITH ETHYLENE TETRAASETIC ACID (EDTA) AS  CAPPING AGENT

By:

Bintang Tunjung Sari

11307141025

Supervisor: Dr. Cahyorini Kusumawardani, M.Si

ABSTRACT

This research aims to determine the effect of variations in the addition of EDTA to particle size and the electronic character of material PbS. PbS nanoparticles with capping agent EDTA has been synthesized by sol-gel method with a precursor Pb (CH3COO-)2 as a source of Pb and (NH4)2S as a source of S and EDTA as a capping agent. The concentration of EDTA is used, are : 0 mmol; 0.1 mmol; 0.2 mmol; 0.5 mmol; 1 mmol. Sol-gel process is performed by stirring CTAB, SDS and EDTA until homogeneous, then added Pb(CH3COO-)2 and (NH4)2S and stirred for 5 minutes to produce black PbS precipitate. The precipitate is filtered and then put into oven at a temperature of 120oC for 3 hours. Results are then used for the synthesis of a thin layer on a glass substrate. XRD results indicate that the structure is cubic PbS, with the size of 8.99 nm, respectively; 2.36 nm; 12.7889 nm; 12.5650 nm and 21.8003 nm. While the results of characterization by UV-Vis band gap energy generating value for PbS/EDTA 3.2 eV, respectively; 3.3 eV; 2.8 eV; 2.8 eV and   2.3 eV.

Key words: nanoparticle, solar cell, EDTA capping agent